Laramie Energy II L.L.C.
Casing and Cement Record

	Well Name       
	Reppo 34-11C
	Date
	November 23, 2009

	Field / Area
	Grand Valley
	Report By
	Cory Claussen


	#
	
	
	
	
	
	
	Overall
	Effective
	Setting
	Depth

	Jts.
	 Size
	  Wt.
	 Gr.
	Cplg.
	Rge.
	Cond.
	Length
	Length
	Set From
	Depth To

	
	
	
	
	
	
	
	
	
	
	

	
	
	
	
	
	
	
	
	-4.54     
	-4.54
	KB

	18
	8-5/8”
	32#
	J-55
	STC
	3
	1
	
	822.32
	KB
	817.78

	1
	Float
	Collar
	
	
	
	
	
	1.00
	817.78
	818.78

	1
	8- 5/8” 
	32#
	J-55
	STC
	3
	1
	
	25.22
	818.78
	844.00

	1
	Float
	shoe
	
	
	
	1
	
	1.00
	844.00
	845.00

	19
	Total Jts.
	
	
	
	
	Total
	845.00


	Casing Crew / Run Time
	Weatherford TRS  Rig up and ran casing 2 hrs.  



	Centralizers
	Middle of  shoe joint  then every other collar to 39’, 

  Total of 10 centralizers.

	Stage 1
	

	Circulation Time / Pres. 
	 Circulate on bottom for 1 hr @ 150#.

	Pre-Flushes
	20 bbls of Fresh water, 


	Cement  Type / Volume
	Lead of 100 sks  Halliburton Versacem System cement, Mixed @ 12.3#/gal, 2.37 yield, 13.76 gal/sk water, Tail of 205 sx Versacem System cement  mixed @ 14.2#, 1.51 yield. 


	Displacement Info.
	47.5 bbls of water

 Bumped Plug to 1080 psi .  Float held.  C.I.P. @ 1220 hrs.  11/23/2009


	Stage 1 Comments
	Returns were full with 10  bbls of cement returns.     

	
	

	1” top job
	None required

	Circulation Time / Pres.
	

	Pre-Flushes
	

	Cement  Type / Volume
	

	Displacement Info.
	

	Stage 2 Comments
	


Mud Properties before Cementing

	9.5+
	80
	27
	26
	20-53
	5.6
	8.7
	8.5
	1250
	11-22-09

	WT.
	VIS
	PV
	YP
	GELS
	WL
	PH
	SOLIDS
	CHLORIDE
	LAST REPORT


Other Remarks

	 Good returns throughout pump dn with 10 bbls cement to surface.  Hole remained full.   

	

	 

	

	


